## Slide 1: TRAINING PROGRAMME FOR IEs
TECHNICAL OFFICERS
Module 7:
Characteristics of typical technological lines in the steel manufacturing industry.

## Slide 2
STEEL PIPE AND GALVANIZED STEEL MANUFACTURING INDUSTRY

## Slide 3
FOCUS ON THE PRODUCTION OF CONSTRUCTION STEEL AND ROLLED STEEL
Reinforcing steel bar
Key products serving the construction industry.
Hot rolled coil (HRC)
Widely used in the manufacturing industry
Structural steel (U, I, H beams)
Applied in construction structures and mechanical engineering
Steel pipe
Used in piping systems and construction

## Slide 4: CONTENT
Features of billet steel production technology
1.1. Blast furnace (BOF) and electric arc furnace (EAF) technology
1.2. Rolling and processing stage
1.3. Integration and synchronization
1.4. Application of advanced technology
1.5. Toward to “green” steel production
1.6. Automation and quality control
1.7. Diverse scale
1.8. Comparison table of energy consumption by technology
Features of pipe steel production technology
2.1. Production line
2.2 heat and surface treatment process
2.3. Welded steel pipe process
3. Utility system
Notes: Hợp đồng hiệu quả năng lượng (EPC): là hợp đồng ký kết giữa ESCO và Khách hàng để thực hiện dịch vụ sử dụng năng lượng tiết kiệm và hiệu quả.
– Hợp đồng chia sẻ mức tiết kiệm năng lượng: ESCO chịu mọi rủi ro tài chính và kỹ thuật của dự án bằng cách thu xếp tài chính để thực hiện dự án đầu tư lắp đặt các trang thiết bị hiệu quả năng lượng tại cơ sở sử dụng năng lượng của khách hàng
– Hợp đồng đảm bảo mức tiết kiệm năng lượng: ESCO chịu trách nhiệm cung cấp, thiết kế, lắp đặt, đo lường và đảm bảo hiệu quả giải pháp sử dụng năng lượng tiết kiệm và hiệu quả cho khách hàng.

## Slide 5
FEATURES OF BILLET STEEL PRODUCTION TECHNOLOGY

## Slide 6
Blast furnace (BOF)
Energy intensityty of BOF in Vietnam is 12.400 MJ/ton
Blast furnace technology, like that of Hoa Phat Group, is a closed chain from iron ore to finished steel. The advantages are low energy consumption and production of high-quality steel with few impurities.
Electric arc fur (EAF)
Energy intensity of EAF in Vietnam is 2.500 MJ/ton
EAF technology is popular among small and medium-sized enterprises, utilizing recycled steel scrap, helping to reduce raw material costs and in line with sustainable development trends.
1. BLAST FURNACE (BOF) AND ELECTRIC ARC FURNACE (EAF) TECHNOLOGY

## Slide 7
1.1. BLAST FURNACE (BOF) TECHNOLOGY
Blast furnace (BOF): Closed production from iron ore to finished steel, allowing for better quality control and
reduced dependence on scrap.
Raw materials for steel production
- Iron ore
Iron ore is the main source of iron, consisting of hematite (Fe2O3) and magnetite (Fe3O4). After mining, iron ore is refined to create concentrate, ensuring the required iron content.
- Coke
Coke is an essential raw material in the ironmaking process, produced from coal through a process of burning in an oxygen-deficient environment. Coke provides heat and acts as a reducing agent in the reduction of iron oxide in the blast furnace.
- Limestone
Limestone (converted into quicklime in a blast furnace)
- Scrap Steel
Alloying elements such as manganese, nickel, chromium, and molybdenum are used to increase the mechanical properties, strength, and wear resistance of steel.

## Slide 8
CHARACTERISTICS OF BLAST FURNACE SYSTEM AT HOA PHAT
 | Information
Number of blast furnaces | Hoa Phat Dung Quat has 4 blast furnaces, each furnace ~1,080m³
Capacity | Total capacity ~5 million tons of pig iron/year
Input materials | Iron ore, coke, limestone
Operating temperature | ~1.800–2.200°C
Control technology | Modern PLC/SCADA automation and control system
Exhaust gas treatment | Has dust collection system, CO, SO₂, NOx gas treatment
Energy recovery | Integrated flue gas heat recovery (WHR) system for internal power generation
Blast furnace technology – BOF converter (BF-BOF route)
Hoa Phat Dung Quat factory uses the traditional steelmaking process from ore with three main stages:
Blast furnace iron smelting
Steelmaking from molten pig iron using converter furnace (BOF)
Finished steel rolling
✅ Advantage:
Produce high quality steel.
Proactive raw materials (ore, coke).
Suitable for large-scale, industrial production.

## Slide 9
Blast furnace system in Hoa Phat
Characteristics of the blast furnace system in Hoa Phat

## Slide 10
Stage | Describe
Sintering | Mix fine ore, coke and additives → form a sinter layer and put it into the blast furnace
Blast Furnace | Fired at ~2,000°C, using coke and hot air → make liquid cast iron
Blast furnace (BOF) | Blowing oxygen into liquid cast iron → reducing C, Si, Mn → into raw steel
Continuous Casting (CC) | Casting cast iron into square workpieces or plates, preparing for rolling
Hot rolling | Hot rolled into steel coils, steel bars, steel pipes...
Main stages
Outstanding technology characteristics
Pulverized Coal Injection System (PCI): Reduce coke consumption, save fuel costs Oxygen Enrichment Technology: Increased Combustion Efficiency and Furnace Smelting Speed Blast Furnace Gas Recovery (BFG): Used to dry raw materials, generate electricity, and make fuel for sintering furnaces SCADA Automation – DCS: Monitoring the operation of the entire production line Continuous Casting & Seamless Hot Rolling: Utilizes billet heat → saves energy
Characteristics of the blast furnace system in Hoa Phat

## Slide 11
Characteristics of the blast furnace system in Hoa Phat
Environmental & Energy Efficiency
Criteria | Typical Values
Coke Consumption | ~450–480 kg/ton cast iron (reduced by PCI)
Heat saving | > 200,000 MWh/year thanks to heat and gas recovery
Reduce CO₂ emissions | ~300,000 tCO₂/year thanks to oxygen + PCI solutions
Rate of reused blast furnace gas | > 90%

## Slide 12
1.2. ELECTRIC ARC FURNACE (EAF) TECHNOLOGY
Electric Arc Furnace (EAF)
Electric Arc Furnace (EAF) Process:
Input materials: Scrap steel, cast iron, DRI (direct reduced iron pellets).
Process:
  Electric Furnace (EAF): Scrap steel is melted by electricity.
  Ladle Furnace: Adjust chemical composition.
  Continuous casting: Create steel billets.
  Hot rolled/cold rolled: Similar process BF-BOF.
Advantage:
  Flexible, suitable for small markets.
  Emission reduction compared to BF-BOF.

## Slide 13
Typical factories using EAF furnaces in Vietnam
Factory | Power | Technology
Pomina | ~1 million tons/year | EAF+CCM (continuous casting)
Vina Kyoei | ~500,000 tons/year | EAF + DRI (blended with scrap)
Southern Steel | ~700,000 tons/year | EAF – Japanese technology
Dana, Việt Đức, SMC steel,... | 200,000–600,000 tons/year | EAF oven – medium
1.2. ELECTRIC ARC FURNACE (EAF) TECHNOLOGY

## Slide 14
Main Specification
Category | Describe
EAF | Capacity 30–120 tons/furnace, brewing time 50–90 minutes/batch
Electrode | Diameter 300–600 mm, consumption 1.5–2.0 kg/ton steel
Material | 80–100% scrap, DRI, or HBI
Refining | LF (Ladle Furnace) Combination to Adjust Chemical Composition
Cooling System | Use water and gas → heat recovery if ORC is integrated
Dust Filtration System | Cloth or electrostatic bags → ensure environmental standards
Criteria | Typical Values
Power Consumption | 580–650 kWh/ton steel
CO₂ emissions | ~0.4–0.6 tCO₂/ton (~70% lower than blast furnace)
Electrode Consumption | 1.5–2.0 kg/ton
Metal recovery rate | 90–95%
Energy efficiency – environment
1.2. ELECTRIC ARC FURNACE (EAF) TECHNOLOGY

## Slide 15
2. ROLLING AND PROCESSING STAGE
Characteristics: Use of modern rolling mills with automatic gauge control (AGC) and X-ray measurement systems to ensure high precision.
Galvanizing technology (NOF– Non-Oxidizing Furnace) is applied to enhance durability and corrosion resistance of cold-rolled steel coils.
Steel products undergo heat treatment (annealing, quenching, tempering) to improve microstructure and mechanical properties.
After steelmaking, steel billets (billet, slab, bloom) are sent to hot rolling or cold rolling mills to produce final products such as coil steel, rebar, structural steel, and steel pipes
Types of rolling | Workpiece temperature | Characteristic
Hot Rolling | > 900°C | Rolling the workpiece while it is still red hot – easy to deform, requires little force
Cold Rolling | Normal temperature | Hot rolled product – high precision, smooth surface
Intermediary Rolling | Between hot and cold | Less common
Energy consumption characteristics
Thermal energy: used for billet furnace – accounts for 60–70% of process energy.
Electricity: operate roller motor, conveyor belt, hydraulic system.
Typical consumption:
  Hot rolling: 2,5–3 GJ/ton
  Cold rolling: 1–1,5 GJ/ton

## Slide 16
The hot rolling process at steel plants in Vietnam typically includes the following main steps:
a. Steel Billet Heating
Billets are fed into a continuous furnace (walking beam furnace) to reach rolling temperature (~1,200°C).
This process ensures the billets have a uniform temperature, making rolling easier and preventing cracking or product defects.
b. Roughing Mill
The heated billets are passed through roughing stands to gradually reduce their initial dimensions.
The product after roughing is in the form of long bars, called transfer bars.
c. Finishing Mill
The transfer bars are further rolled in the finishing mill system to achieve the desired size and shape (plates, coils, bars, etc.).
At this stage, rolling speeds are very high, requiring precise automatic control systems.
d. Cooling (Cooling Bed or Laminar Cooling)
After rolling, steel products are rapidly cooled either on a cooling bed (for construction steel) or through a forced cooling system (for hot rolled coils).
e. Coiling and Cutting
For coil products, the material is wound into coils using coiling equipment.
For bar products, the steel is cut to specified lengths and bundled.
2. ROLLING AND PROCESSING STAGE

## Slide 17
Some Typical Steel Plants in Vietnam with Hot Rolling Processes
Hoa Phat Group – Dung Quat Steel Plant: Large-scale HRC (Hot Rolled Coil) production.
Formosa Ha Tinh Steel Corporation: Integrated process from ironmaking – steelmaking – hot rolling – cold rolling.
Southern Steel Company – VNSTEEL: Rolling construction steel products.
Pomina Steel Corporation: Owns modern rolling lines for rebar production.
Some Typical Steel Plants in Vietnam with Cold Rolling Processes
Hoa Sen Group: Cold rolling combined with galvanizing and color coating lines.
Dong A Steel Joint Stock Company: Supplier of high-quality CRC, GI, and GL products.
POSCO Vietnam (Ba Ria – Vung Tau): Modern cold rolling line producing steel products for the export industry.
Hoa Phat Group: Invested in modern cold rolling lines to serve the coated steel industry.
2. ROLLING AND PROCESSING STAGE

## Slide 18
Cold Rolling Process
The standard cold rolling process in Vietnamese steel plants typically includes the following steps:
a. Pickling
Hot Rolled Coils (HRC) are cleaned of the oxide layer (rust) using acid (HCl or H₂SO₄) to prepare for cold rolling.
Ensures a clean steel surface, free of impurities that could affect rolling quality and subsequent coating.
b. Cold Rolling Mill
After pickling, the steel coil is fed into the cold rolling mill (usually 4-high or 6-high mills).
Thickness is reduced from 1.5–3 mm down to 0.15–1.5 mm with high precision.
Increases hardness and internal stress of the material.
c. Annealing
After rolling, the steel has high hardness and is difficult to process.
The annealing process (Batch Annealing or Continuous Annealing) restores ductility and stabilizes the crystal structure.
d. Skin-pass or Temper Rolling
Enhances surface brightness, ensures uniform thickness, and removes minor folds.
Improves adhesion for galvanizing or coating.
e. Edge Trimming, Recoiling, and Quality Inspection
Finished coils are edge-trimmed, recoiled to specification, labeled, and transferred to the finished goods warehouse.
2. ROLLING AND PROCESSING STAGE

## Slide 19
3. INTEGRATION AND SYNCHRONIZATION
Value chain optimization
Large-scale technology lines are designed in a synchronized manner, from raw material processing to ironmaking, steelmaking, and finished steel rolling.
Waste reduction
A closed-loop system helps reduce waste and increase production efficiency. CO gas from the blast furnace is recovered and reused as fuel.
Production efficiency
Integrating production stages helps optimize the process and reduce production costs.

## Slide 20
4. APPLICATION OF ADVANCED TECHNOLOGY
Technology import
Many steel production lines in Vietnam are imported from countries with developed steel industries such as Italy, Japan, or South Korea.
Automation
The steel rolling lines use high automation technology, ensuring accuracy and product quality
Accuracy
Advanced technology helps produce steel with high accuracy, meeting international standards

## Slide 21
5. TOWARD TO “GREEN” STEEL PRODUCTION
Emission reduction
Vietnam's steel industry is adjusting its production lines to reduce emissions and meet international standards
Renewable energy
Using renewable energy to reduce carbon emissions
Coal gasification
Using coal gasification instead of FO oil to reduce pollution
Scrap recycling
  Enhancing steel scrap recycling in the EAF production line.

## Slide 22
6. AUTOMATION AND QUALITY CONTROL
100%
Automation
Modern technological line integrated with automation system (PLC).
Advanced
Measuring equipment
Advanced measuring equipment is used (such as X-ray thickness gauges).
International
Standard
Ensure the products meet international standards (JIS, ASTM, TCVN).

## Slide 23
7. DIVERSE SCALE
Large Enterprise
Own a large-capacity production line (millions of tons per year)
Small Factory
Focus on producing specialized steel or serving local demand.
Design Capacity
Ranging from 250,000 tons per year to 8 million tons per year

## Slide 24
8. COMPARISON TABLE OF ENERGY CONSUMPTION BY TECHNOLOGY
Technology | Actual level in Vietnam | Advanced level (EU, Japan)
BF – BOF | 22–28 GJ/ton of steel | 18–20 GJ/ton
EAF | 500–650 kWh/ton | < 400 kWh/ton
Compare with international advanced level (benchmark)
Steel Production Technology | Main Raw Materials | Energy Consumption Rate | Notes
Blast Furnace – Basic Oxygen Furnace (BF-BOF) | Iron ore, coke | 20–30 GJ/ton of steel (~5,500–8,300 kWh/ton) | Traditional technology, high CO₂ emissions
Electric Arc Furnace (EAF) | Scrap steel | 350–650 kWh/ton | Electricity-intensive, lower CO₂ emissions, more environmentally friendly
Induction Furnace (IF) | Scrap steel | 550–750 kWh/ton | Common in small plants, lower efficiency than EAF
Hòa Phát (modern BF) | Iron ore, coke | ~20–22 GJ/ton of pig iron (~5,500–6,100 kWh) | Includes furnace heat recovery, ISO 50001 certified
Pomina (improved EAF) | Scrap steel | ~500–550 kWh/ton | Integrated energy monitoring, optimized electrode usage

## Slide 25: Q & A
What solutions has your factory applied to reduce energy consumption? Please share the experiences that your factory has applied.

## Slide 26
2. CHARACTERISTICS OF STEEL PIPE
PRODUCTION TECHNOLOGY

## Slide 27
Hot Rolling Process
1. Material Loading
2. Flattening
3. Roughing Mill
4. Slitting
5. Roughing Mill
6. Tensioning
7. Coiling
8. Material Unloading
2.1. PRODUCTION LINE
Descaling Process
1. Material Loading
2. Pickling Tank 1
3. Pickling Trough
4. Rinsing Trough
5. Drying
6. Tensioning 1
7. Pickling Tank 2
8. Tensioning 2
9. Coiling
10. Material Unloading

## Slide 28
Cold Rolling Process
1. Material Loading
2. Pickling Tank
3. Stand 1
4. Stand 2
5. Stand 3
6. Stand 4
7. Coiling
8. Material Unloading
Annealing Process
1. Material Loading
2. Roughing Mill 1
3. Annealing Furnace
4. Rapid Cooling
5. Annealing Tank
6. Rapid Cooling Tower
7. Roughing Mill 2
8. Coiling
9. Material Unloading
Pipe Making Process
1. Uncoiling
2. Pickling Tank
3. Forming Roll Stand
4. High-Frequency Welding
5. Shaping Roll Stand
6. Cutting Table
7. Pipe Collection
8. Bundling
2.1. PRODUCTION LINE

## Slide 29
2.2 HEAT AND SURFACE TREATMENT PROCESS
Heat Treatment
Heat treatment (annealing, quenching, tempering) is carried out thoroughly to improve the mechanical properties of the steel.
Surface Plating
Surface plating technology (galvanizing) to increase durability and corrosion resistance.
Process | Target | Characteristic
Annealing | Reduce hardness, increase flexibility | Cool slowly in the furnace
Quenching | Increase hardness | Cool quickly after firing
Tempering | Tempering after quenching | Reheat at low temperature (150–650°C)
Normalizing | Improving microstructure | Air cooled
Carburizing, Nitriding | Increase surface hardness | Chemical and thermal combination
Typical heat treatment processes

## Slide 30
Surface Plating: Surface plating technology (galvanizing) to increase durability and corrosion resistance.
1. Degreasing
Target: Remove grease and dirt on steel surface.
Method: Use alkaline solution (NaOH) or organic solvent.
Note: If not cleaned thoroughly, the plating will not adhere firmly.
2. Pickling
Target: Remove rust (iron oxide) from steel surface.
Method: Soak in dilute acid solution, usually HCl or H₂SO₄.
Cleaning time: 5–20 minutes, depending on rust thickness.
3. Water Rinse
Target: Remove residual acid after pickling step.
Rinse with clean water and drain before moving on to the next step.
4. Fluxing
Target: Create a thin coating (ZnCl₂ – NH₄Cl) to support better zinc adhesion and prevent temporary oxidation.
Method: Dip in saline flux solution.
5. Hot-dip Galvanizing
Target: Dip steel into molten zinc bath (~450°C).
Application: Zinc and iron form a metal-metal reaction bond - Fe-Zn alloy, very good corrosion resistance.
Dipping time: depends on product thickness.
6. Cool and test
Cool with air, water or special solution.
Check plating layer: thickness, adhesion, surface (according to JIS, ASTM or TCVN standards).
Can be passivated to increase rust resistance (if required).
2.2 HEAT AND SURFACE TREATMENT PROCESS

## Slide 31
2.3 WELDED STEEL PIPE PROCESS
Electric Resistance Welding (ERW) Steel Pipe Production Process
The Electric Resistance Welding (ERW) technology is the most widely used in Vietnam today. The standard process includes:
a. Slitting
Steel coils are slit into strips with widths suitable for each pipe size.
b. Forming
Steel strips are fed into a forming mill, where rollers gradually shape them into a round (or square, rectangular) tube.
c. Welding
The edges of the steel strip are joined using high-frequency electric resistance welding (HF-ERW).
No filler material is used; the weld seam is tightly forged, ensuring a strong bond.

## Slide 32
d. Cooling and Weld Cleaning
Cooling with water or air.
Excess weld material inside/outside the pipe is removed using scrapers or lathes.
e. Sizing
Pipes are passed through sizing rollers to refine shape and adjust dimensions.
f. Cutting and Inspection
Pipes are cut to standard lengths (commonly 6m).
Visual and dimensional inspections are conducted.
For higher requirements, ultrasonic testing (UT) or hydrostatic testing may be performed.
g. Galvanizing or Painting (if applicable)
Some plants integrate hot-dip galvanizing or electro-galvanizing lines to enhance product durability.
2.3 WELDED STEEL PIPE PROCESS

## Slide 33
Category | Typical Consumption | Notes
Total Power Consumption | 80 – 150 kWh/ton of steel pipe | Depends on thickness, size
Specific power consumption for welding | 20 – 40 kWh/ton | High-frequency resistance welded
Total Consumption Coefficient (TOE/ton SP) | 0.015 – 0.035 TOE/ton | Equivalent to 63 – 147 kWh/ton
Reference energy consumption
(*TOE: Tonne of Oil Equivalent, 1 TOE ≈ 4,187 GJ ≈ 1,163 MWh)
2.3 WELDED STEEL PIPE PROCESS

## Slide 34
Energy Consumption Hotspot Analysis
2.3 WELDED STEEL PIPE PROCESS
System | Description | Saving Potential (%)
HF High-Frequency Welding Machine | Consumes large amounts of electricity, especially at high loads | 10–15% if replaced with IGBT
Drive System (Motor) | Old motors, running continuously without load | 10–30% if using inverters (VFDs)
Cooling System | Pumps and fans run continuously, not load-based | 10–20% if pumps/fans are optimized
Slitting Workshop | Uses many motors, direct start-up | 5–15% if start-up sequence is optimized
Compressed Air & Lighting | Air leakage, old lamps, excessive lighting | 5–10% if using LEDs and controlling compressed air

## Slide 35: 3. UTILITY SYSTEM
3.1 Heat supply system and furnace
Induction kiln (billet steel) / Heating furnace (hot-rolled tube steel): Increase the temperature of the billet or coil to 1200–1300°C.
Auxiliary equipment: Combustion equipment, heat controller, chimney – exhaust fan.
3.2 Hydraulic system – lubrication
3.3 Water supply and cooling system
Cooling water circulation system: Cooling workpieces, furnaces, large motors. Inlet water treatment system: Removal of sediment, ions – protection of thermal equipment.
Hydraulic system: Provides control force to mechanical equipment. Lubrication system: Reduce friction, increase the life of the rotating equipment.

## Slide 36: 3. ENERGY SUPPLY SYSTEM
Power substation and distribution cabinet: Supply power to the whole plant. SCADA/PLC control system: Automation, process monitoring.
3.4 Electrical – Control System
3.5 Fuel and gas systems
Gas supply system: Supply NG, CO/H2 gas, blast furnace gas. Oxygen supply system, inert gas: Used in steelmaking and welding.
3.6 Compress air system
Supply compressed air to actuators, valves, cleaning equipment.
3.7 Ventilation – vacuum – inert gas treatment system
Dust extraction system: Suction of smoke and dust from furnaces, welders, rolling machines. Exhaust gas treatment system: SO2, NOx, CO, fine dust treatment.

## Slide 37: 3. ENERGY SUPPLY SYSTEM
3.8 Laboratory Systems – Testing
Product quality assurance: chemical, mechanical, ultrasonic testing,...
3.9 Other systems
System | Main Function
Fire Protection System | Fire and explosion warning, fire suppression using water, foam, CO₂ gas
Thermal Load Balancing System | Utilize excess heat – heat exchange between workshops
Internal Transportation System | Forklifts, trolleys, overhead cranes for transporting billets, steel coils, etc.
Storage and Packaging System | Preserve and transport steel billets/pipes to customers

## Slide 38: Q&A
1: What’s the difference between BOF and EAF in steel production?
2: Why are many countries shifting from BOF to EAF?
3: What is the difference between hot rolling and cold rolling in steel processing?
4: What are the environmental challenges of old steel technologies?

## Slide 39
THANK YOU