## Slide 1: TRAINING PROGRAMME FOR IEs
Technical Staffs
Module 7:
Introducing typical technological line characteristics in cement production line

## Slide 2
CEMENT INDUSTRY

## Slide 3
INFORMATION ON TYPICAL TECHNOLOGICAL LINE CHARACTERISTICS
SOME TECHNOLOGICAL LINE CHARACTERISTICS IN CEMENT PRODUCTION LINE
CONTENT

## Slide 4
I. INFORMATION ON TYPICAL TECHNOLOGICAL LINE CHARACTERISTICS

## Slide 5: GENERAL INFORMATION
Main production field: Cement and clinker production
Main products: Clinker, PCB 30 cement, PCB 40 cement
Production scale: 1 cement production line with a capacity of 4,000 tons of clinker per day
Key energy equipment: Transformer station, air compressor station, circulating pump station...

## Slide 6: PRODUCTION LINE
Cement production process
Production process
Basic production process:
Raw material extraction (limestone, clay, additives)
Grinding, mixing raw materials
Burning clinker at ~1,450°C
Cooling clinker
Grinding clinker with additives (gypsum, mineral additives) to produce cement

## Slide 7: PRODUCTION LINE
Types of energy used in the chain:
Coal is used for the clinker burning process in the kiln.
Electricity is used in systems and equipment such as: Crushers, grinders, fan systems, dust filters, bagging, air conditioning, lighting, air compressors, etc.
The compressed air distribution system provides compressed air for the control of pistons in production machines and dust filters, bagging, and kilns.
FO oil is used for the kiln start-up process and additional burning when necessary.

## Slide 8
II. SOME TECHNOLOGICAL LINE CHARACTERISTICS IN CEMENT PRODUCTION LINE

## Slide 9
1. DRY ROTARY KILN TECHNOLOGY
Advantage
Reduce fuel consumption (coal, electricity)
Increase production
Reduce greenhouse gas emissions
Prevail
Dry rotary kiln technology is the most popular technology in the Vietnamese cement industry today, accounting for the majority of production plants.
This technology uses a dry rotary kiln with a pre-heating and pre-calcining system, which saves energy and increases efficiency compared to traditional vertical kiln technology.

## Slide 10
Vicem Hoang Thach Cement: One of the pioneering plants applying rotary kilns in Vietnam, with large capacity and modern production lines. This plant is located in Hai Duong province and produces about 1.6-1.8 million tons of cement per year.
Nghi Son Cement: A joint venture between Vietnam and Japan, using a rotary kiln with a capacity of 5,800 tons of clinker per day, it is one of the largest plants in the country.
But Sơn Cement (Vicem But Son): Located in Ha Nam, with a capacity of about 4,000-5,000 tons of clinker per day, producing over 1.6 million tons of cement per year.
Ha Tien Cement (Vicem Ha Tien): A plant in Ho Chi Minh City and surrounding provinces, using modern rotary kilns, with an annual output of millions of tons.
Cam Pha Cement: A plant in Quang Ninh, applying the dry rotary kiln method, with a capacity of about 2.3 million tons of cement per year.
The Vissai Cement: A large group in Ninh Binh, with many rotary kiln production lines, with a total output of up to 13 million tons of cement per year.
Duyen Ha Cement: Located in Ninh Binh, with a rotary kiln capacity of about 4,000-5,000 tons of clinker per day, producing products that meet international standards.
1. DRY ROTARY KILN TECHNOLOGY

## Slide 11
Current Situation and Trends Modernization: Many plants are investing in waste heat recovery technologies to generate electricity, reduce CO₂ emissions, and improve efficiency. For example, Hoang Thach and Nghi Son Cement Plants have implemented such solutions.
Challenges: Although dry-method rotary kilns are less polluting than vertical kilns, plants still face issues with fine dust and gas emissions (SO₂, NOₓ, CO₂), requiring advanced environmental treatment systems.
Overview Statistics: As of now, Vietnam has around 80 cement plants of various sizes, with over 50% using rotary kilns and a total designed capacity exceeding 100 million tons per year. The actual production in 2024 is estimated at around 90–100 million tons, meeting both domestic demand and export needs.
1. DRY ROTARY KILN TECHNOLOGY

## Slide 12
AVERAGE ENERGY CONSUMPTION RATE
Thermal Energy
The average thermal energy consumption for producing 1 kg of clinker in Vietnam ranges from 730 to 850 kcal/kg of clinker. Plants using modern dry-method rotary kilns typically achieve the lower end of this range.
Electricity
The energy consumption rate for producing 1 ton of cement ranges from 90 to 110 kWh/ton of cement. Modern plants with highly automated systems can reduce it to below 90 kWh/ton of cement.
Energy consumption rate is an important indicator reflecting the efficiency of energy use in the cement production process. Reducing energy consumption rate not only helps factories save costs but also contributes to environmental protection.

## Slide 13
COMPARE WITH INTERNATIONAL STANDARDS
National Goals
The Vietnam Building Materials Development Strategy for the 2021–2030 period sets a target of thermal energy consumption ≤ 730 kcal/kg of clinker and electricity consumption ≤ 90 kWh/ton of cement.
Approaching the standard
Many large factories in Vietnam have approached or nearly achieved these targets thanks to the adoption of advanced technologies. However, there are still some small or outdated plants that have not yet reached optimal consumption levels.
Distance
The average consumption levels of Vietnam’s cement industry are still higher compared to developed countries such as Japan (650–700 kcal/kg of clinker and 80–85 kWh/ton of cement).
Comparing with international standards helps us better understand the position of Vietnam’s cement industry on the global energy map and highlights the efforts needed to achieve higher efficiency.

## Slide 14
CURRENT SITUATION AT SOME TYPICAL FACTORIES
This comparison table shows clear differences between plants in energy efficiency, depending on technology and production scale.
Factory | Thermal Energy (kcal/kg clinker) | Electricity (kWh/ton of cement)
Nghi Son Cement | 730–750 | 85–90
Hoang Thach Cement | 760–800 | 90–95
INSEE Hon Chong Cement | 700–730 | N/A
Small factory (<2,500 tons/day) | 850–950 | 100–120

## Slide 15
FACTORS AFFECTING ENERGY CONSUMPTION RATE
Production technology
Dry-method rotary kilns with preheater towers and precalciners significantly reduce thermal energy consumption.
Fuel used
Coal dust is the main fuel, accounting for about 80-90% of thermal energy. Some factories have started using alternative fuels.
Factory size
Large-capacity plants typically have lower energy consumption rates than small plants.
Maintenance and Management
Regular maintenance and optimization of operating procedures also have a major impact on energy efficiency.
These factors are closely related to each other and optimizing each factor will bring about an overall effect in reducing energy consumption.

## Slide 16
By 2025, 100% of cement production lines with a capacity of 2,500 tons of clinker/day or more will be required to install a power generation system that utilizes waste heat, helping to reduce electricity costs by 25-30%(*)
Working principle
The WHR system uses waste heat from:
  Clinker kiln gas: ~300–400°C
  Cooler gas emissions: ~250–350°C
This heat is recovered to generate steam (or thermal oil), which is fed into a steam turbine or ORC (Organic Rankine Cycle) to generate electricity.
2. WASTE HEAT UTILIZATION
(*) Decision No. 1488/QD-TTg dated August 29, 2011 of the Prime Minister approving the Vietnam Cement Industry Development Plan for the 2011-2020 period and vision to 2030.

## Slide 17
2. Popular configurations
Steam Rankine Cycle:
  Waste Heat Boiler
  Steam turbine – generator
  Water treatment system, condenser, high-pressure pump
Organic Rankine cycle – applicable for lower temperature exhaust gases (~200–300°C)
2. WASTE HEAT UTILIZATION

## Slide 18
Category | Reference value
Heat recovery | 15–20% of total heat input
Power generation efficiency | 20–30 kWh/ton clinker
Unit capacity | 4 – 10 MW (factory scale 5,000 – 10,000 tons of clinker/day)
Internal power self-sufficiency rate | 20 – 30% of the entire factory's electricity needs
Specific investment | 2.0 – 2.5 million USD/MW
Payback period | 3 – 5 years (depending on electricity price and operating load)
3. Power and efficiency
2. WASTE HEAT UTILIZATION

## Slide 19
3. USE ALTERNATIVE FUELS
Alternative raw materials
Blast furnace slag, fly ash from thermal power plants
Alternative fuels
Industrial waste, rice husks, plastic scrap
Many cement factories in Vietnam have adopted the use of alternative fuels and raw materials to reduce costs and environmental impacts. For example, some factories utilize ash from coal-fired thermal power plants as an additive in clinker production.

## Slide 20
Factory | Estimated average AFR | Alternative fuel type
INSEE (formerly Holcim) | > 30% | RDF, rubber, plastic, rags
Nghi Son Cement | ~10% | RDF, industrial sludge
Xuan Thanh Cement | ~8% | Garbage, rags
Vicem Hoang Thach | < 5% | Rice husk, waste oil
Many other Vicem factories | < 2% | Use the test
🔎 Industry average: Alternative energy usage rate - AFR: under 5%, while the target by 2030 is 15–20% according to the Construction Materials Development Strategy.
Difficulties and barriers
There is no standardized waste classification and treatment system to provide stable RDF.
Furnace technology needs to be adapted to simultaneously burn many types of fuels with different moisture and calorific values.
Fuel preparation (drying, grinding, mixing) is complicated and requires large investment.
Environmental permitting issues, concerns about odor and toxic emissions
3. USE ALTERNATIVE FUELS

## Slide 21
4. AUTOMATION AND CENTRAL CONTROL
Optimization
Production process
Monitor
Product quality
Reduce
Human error
Modern production lines are often equipped with highly automated and central control systems that optimize production processes, monitor quality, and minimize human error. This technology also supports real-time monitoring of emissions and energy consumption.

## Slide 22
VICEM Hoang Thach: This plant has applied advanced automation systems and is moving towards integrating AI to optimize rotary kilns and energy management. The waste heat power generation system is also supported by smart data analytics tools.
Nghi Son Cement: With Japanese technology, this plant uses smart control systems that can integrate AI to reduce energy consumption to 730-750 kcal/kg of clinker and optimize rotary kiln operations.
The Vissai Cement: This group is investing in modern technology, including automation and data analytics solutions, which could be the foundation for AI deployment soon.
4. AUTOMATION AND CENTRAL CONTROL

## Slide 23
AI technology is popular in cement factories
Machine Learning - ML: Use algorithms like Gradient Boosting and Neural Networks to predict product quality or optimize processes.
Artificial Neural Networks - ANN: Applied to simulate complex processes such as clinker firing or cement grinding.
Advanced Process Control - APC: Combine AI with traditional control systems to automate operational decisions.
IoT: Connect sensors and devices in the factory to collect Big Data, providing a platform for AI analysis.
Digital Twin: Create digital models of rotary kilns, mills or entire production lines for testing and optimization without affecting actual operations.
4. AUTOMATION AND CENTRAL CONTROL

## Slide 24
5. VERTICAL ROLLER MILL TECHNOLOGY
Convert
From ball mill to vertical roller mill
Application
Grinding of raw materials, coal and cement
Effective
Saving electricity and increase grinding efficiency
Many factories have switched from ball mills to vertical roller mills for grinding raw materials, coal, and cement. This technology saves electricity and increases grinding efficiency.

## Slide 25
6. LARGE PRODUCTION LINE CAPACITY
4.000 - 6.000
Tons of Clinker/Day
Typical capacity
International Standards
Design
Suitable for needs
Modern production lines in Vietnam often have a capacity of 4,000 - 6,000 tons of clinker/day, even designed according to international standards, suitable for large domestic and export cement consumption needs.

## Slide 26
7. AUXILIARY SYSTEM
Power Supply System
Characteristics: Supplies energy to all equipment in the plant, including rotary kilns, grinders, fans, lighting systems, and other auxiliary devices.
Features: Ensures stable and reliable electricity distribution, especially in large plants with high-capacity equipment. Some plants use backup generators to maintain critical systems during grid power outages.
2. Compressed Air System
Characteristics: Provides compressed air for control systems and operates automated equipment such as valves, pumps, and fans.
Features: Compressed air systems in cement plants in Vietnam typically use high-capacity compressors (100–250 kW) capable of supplying stable compressed air. Energy savings are achieved by using variable frequency drives (VFDs) to control compressor power.

## Slide 27
7. AUXILIARY SYSTEM
3. Water System
Characteristics: Supplies water for cooling, drying, equipment cleaning, and domestic use within the plant.
Features: Water systems in Vietnamese cement plants commonly reuse water from cooling processes and wastewater treatment, helping reduce costs and protect the environment.
4. Exhaust Gas and Dust Treatment System
Characteristics: Cement plants in Vietnam often use bag filters, cyclones, or exhaust fans to remove dust and gases generated during production.
Features: Ensures compliance with environmental regulations, reduces air pollution, and protects worker health.

## Slide 28
7. AUXILIARY SYSTEM
5. Cooling System
Characteristics: Responsible for cooling equipment such as rotary kilns, grinders, and other components in the plant.
Features: Uses cooling water or cooling fans to maintain stable temperatures during production, reducing the risk of equipment failure and improving energy efficiency.
6. Automation and Control System
Characteristics: Modern cement plants in Vietnam typically use automated control systems (PLC, SCADA) to monitor and manage production processes.
Features: Enhances management efficiency, reduces incidents, and saves energy by adjusting operational parameters such as temperature, pressure, and flow rate.
7. Fuel System
Characteristics: Uses coke or fuel oil (FO) as the main fuel for clinker burning in rotary kilns.
Features: Fuel systems typically include fuel storage tanks and pumps to distribute fuel efficiently and economically.

## Slide 29
8. MAINTENANCE EFICIENCY
Grinding system (Ball mill, vertical mill)
Check and replace grinding balls, rollers, grinding table when worn beyond the limit → avoid reducing grinding efficiency.
Adjust clearance, hydraulic pressure to ensure reasonable compression.
Clean the separator → avoid coarse particles to increase grinding cycle.
Check the tightness of the system → avoid loss of hot air and dust.
2. Industrial fans & dust filters
Dynamically balance the fan, clean the fan blades → reduce vibration, reduce mechanical loss.
Check the bearing clearance, lubricate periodically.
Measure and adjust the pressure and flow to avoid overloading.
Maintain bag dust filters, electrostatic dust filters → reduce air flow obstruction.

## Slide 30
8. MAINTENANCE EFICIENCY
3. Clinker kiln
Check the tightness of the kiln door gasket, rotary valve → avoid cold air from entering, reduce the temperature of the combustion chamber.
Clean the heat exchange surface in the pre-burning tower → limit the adhesion causing increased heat loss.
Maintain the coal supply system, pilot oil → ensure stable fuel injection, optimal combustion.
4. Air compressor
Check for air leaks (at joints, pipes, valves) → each 2 mm leak can lose 2–3 kW of electricity.
Maintain air filter, oil filter → avoid reducing compression efficiency.
Adjust pressure according to actual needs, avoid running over pressure.

## Slide 31
8. MAINTENANCE EFICIENCY
5. Conveyor & motor system • Align shaft, grease bearings, reduce friction. • Check belt tension, rollers, avoid mechanical loss. • Measure motor current, detect underload or overloaded motor → adjust or replace with high-efficiency motor.
6. Modern maintenance techniques
Predictive Maintenance uses:
Vibration and temperature sensors (Condition Monitoring).
IoT & SCADA to monitor motor, fan, and crusher performance online.
Use CMMS (Computerized Maintenance Management System) to plan and track maintenance schedules.
Benefits
Reduces power consumption by 3–8% for rotating equipment (fans, motors, grinders).
Reduces heat consumption by 1–3% for the furnace system.
Extends equipment life, reduces major repair costs. • Increases product stability and quality.

## Slide 32: DISCUSSION
Question 1: Based on the technological characteristics, please state the energy saving opportunities that can be applied to your factory.
Question 2: Please review the factory's auxiliary system, find and make discoveries about the potential?

## Slide 33
THANK YOU